## Slide 1: osscar-quantum-mechanics.materialscloud.io github.com/MosaicGroupCMU/African-MRS-Tutorials

## Slide 2: Vibrational modes and infrared spectra
Lorenzo Bastonero
Nicola Marzari
AMRS, Workshop
„Introduction to Computational Materials Science“

## Slide 3
Liquid
Solid
Gas
From DFT

## Slide 4: What controls?
Temperature
Thermal expansion
Phase transition & Dynamical stability
Heat transport
Transport coefficients

## Slide 5: How can we study ?

## Slide 6: Atomic interactions as springs

## Slide 7: The harmonic approximation
= 0
constant
= force const.
oscillation frequency
Same approach as for the pendulum
Small angle  small (atomic) oscillations

## Slide 8: Normal modes and vibrational frequencies
phonons
periodic
vibrons
molecular
Number of frequencies = Number of degree of freedom
Interatomic Force Constant (IFC) matrix
For water: (3 atoms) x (3 directions) – (3 translations) – (2 rotations) – (1 reflection/mirror) = 3 !

## Slide 9: Dynamical stability
Stable
Unstable

## Slide 10: Vibrations in solids

## Slide 11: Phonon dispersion
Acoustic
IR/Raman
Optical
Inelastic Neutron Scattering (INS)
Dynamical
matrix

## Slide 12: Examples: Si and Ge
P. Giannozzi et al., Phys. Rev. B, 43, 9 (1991)

## Slide 13: How to compute phonons?
Frozen phonons (finite displacements)
Linear response (DFPT)
New set of self-consistent equations
To solve in primitive cell for each q
Calculates D(q)
To compute in supercell

## Slide 14: Interaction with light
Electromagnetic range where ions respond: 0–1012 Hz

## Slide 15: Infrared absorption
Born effective charges
Oscillator strength
Vibration eigenvector

## Slide 16: Example: water
Credit: https://www.azom.com/article.aspx?ArticleID=22517

## Slide 18: Example: amorphous silica (SiO2)
L. Giacomazzi et al., Phys. Rev. B, 79, 064202 (2009)

## Slide 19: Nature of the interactions
Long range
(polar semiconductors)
Short range
(homopolar semiconductors, metals)

## Slide 20: Long-wavelength vibrations in polar materials
Transverse optical (TO)
Longitudinal optical (LO)
Coupling with macroscopic electric field  frequency shift (or splitting):

## Slide 21: Examples: GaAs and AlAs
Baroni, S. et al., Rev. Mod. Phys., 73, 515 (2001)

## Slide 22: Summary
The potential energy surface E({R}) is responsible for many different observables.
The harmonic approximation provides information on the dynamics and stability of the system.
In solids, there are infinite frequencies described in Fourier space by a phonon dispersion.
The vibrational modes can be observed using interaction with light (IR).
Vibrational modes and IR absorption can be computed using DFT coupled with more advanced techniques (finite differences, DFPT).

## Slide 24: How to compute infrared intensities?

## Slide 25: Long-wavelength vibrations in polar materials
Baroni, S. et al., Rev. Mod. Phys., 73, 515 (2001)