## Slide 1: Vibrational modes and infrared spectra
Lorenzo Bastonero
Nicola Marzari
AMRS, Workshop
„Introduction to Computational Materials Science“

## Slide 2
Liquid
Solid
Gas
From DFT

## Slide 3: What controls?
Temperature
Thermal expansion
Phase transition & Dynamical stability
Heat transport
Transport coefficients

## Slide 4: The harmonic approximation
= 0
constant
= force const.
oscillation frequency
Same approach as for the pendulum
Small angle  small (atomic) oscillations

## Slide 5: Normal modes and vibrational frequencies
phonons
periodic
vibrons
molecular
Number of frequencies = Number of degree of freedom
Interatomic Force Constant (IFC) matrix
For water: (3 atoms) x (3 directions) – (3 translations) – (2 rotations) – (1 reflection/mirror) = 3 !

## Slide 6: Dynamical stability
Stable
Unstable

## Slide 7: Vibration in solids

## Slide 8: Phonon dispersion
Acoustic
IR/Raman
Optical
Inelastic Neutron Scattering (INS)
Dynamical
matrix

## Slide 9: Examples: Si and Ge
P. Giannozzi et al., Phys. Rev. B, 43, 9 (1991)

## Slide 10: How to compute phonons?
Frozen phonons (finite displacements)
Linear response (DFPT)
New set of self-consistent equations
To solve in primitive cell for each q
Calculates D(q)
To compute in supercell

## Slide 11: Interaction with light
Electromagnetic range where ions respond: 0–1012 Hz

## Slide 12: Infrared absorption
Born effective charges

## Slide 13: Examples: amorphous silica (SiO2)
L. Giacomazzi et al., Phys. Rev. B, 79, 064202 (2009)

## Slide 14: Nature of the interactions
Long range
(polar semiconductors)
Short range
(homopolar semiconductors, metals)

## Slide 15: Long-wavelength vibrations in polar materials
Transverse optical (TO)
Longitudinal optical (LO)
Coupling with macroscopic electric field  frequency shift (or splitting):

## Slide 16: Example: GaAs and AlAs
Baroni, S. et al., Rev. Mod. Phys., 73, 515 (2001)

## Slide 17: Summary
The potential energy surface E({R}) is responsible for many different observables.
The harmonic approximation provides information on the dynamics and stability of the system.
In solids, there are infinite frequencies described in Fourier space by a phonon dispersion.
The vibrational modes can be observed using interaction with light (IR).
Vibrational modes and IR absorption can be computed using DFT coupled with more advanced techniques (finite differences, DFPT).

## Slide 19: How to compute infrared intensities?

## Slide 20: Long-wavelength vibrations in polar materials
Baroni, S. et al., Rev. Mod. Phys., 73, 515 (2001)